## Slide 1: Direct Fabrication of Low-Temperature Co-fired Ceramics (LTCC) Circuits
Wenbin Li,
Austin Martin,
6/12/2018

## Slide 2
LTCCs in vehicle EPS *
(electric power steering)
LTCCs in high frequency wireless modules
LTCC and HTCC, and their applications
https://www.youtube.com/watch?v=oYLQc-uVClE&t=50s

## Slide 3
Conventional LTCC/HTCC fabrication process
https://www.youtube.com/watch?v=N85Tx_7HPZs&t=17s

## Slide 4
Convectional tape-stacking way of fabricating LTCCs
Direct fabrication by AM

## Slide 5
G-Code preview: Printing a LTCC circuit board for lightening 5 LEDs
Direct fabrication of LTCC by AM

## Slide 6: Outline
Introduction LTCC LTCC and its application Conventional way of LTCC fabrication
Direct fabrication of LTCC Demonstration of LTCC direct fabrication Work flow of LTCC direct fabrication
Challenges and issues

## Slide 7
Demonstration of LTCC printing:
White material – ZrO2 paste
Green material – Al2O3 paste with ~1wt% of Cr2O3

## Slide 8
‘Green’ state
Sintered

## Slide 9
Step 1- Design PCB file in Altium Designer
Step 2- Convert PCB file into multiple STL files in ACE Translator
Work flow of LTCC direct fabrication

## Slide 10
Stacked STL models (dielectric layers excluded)
Step 3- Generate FDM-style G-Code in Simplify3D

## Slide 11
Tool-1: Base layer (ceramic)
Tool-2: Dielectric layers (ceramic)
Tool-3: Conductive film (traces, pads, metal)
Tool-4: Via-filling (metal)

## Slide 12
Step 4- Convert G-Code FDM-style to CODE-style using a converting program
Step 5- Print, dry and sinter

## Slide 13
Challenges:
Limitations on dimensional resolution and accuracy
Thin paste spread out after being deposited,
making it difficult to form via holes
with small diameter.
The issue was mitigated by using
paste with higher viscosity
The pastes’ spreading behavior for straight lines and curvature line need to be investigated to
achieve precise control of the via hole size and trace width.

## Slide 14
2. Nozzle clogging
One nozzle working,
the other one being idle
and easily get clogged on-the-fly
Solution:
Extruder A finished one layer
Nozzle A&B moved into solvent
Extruder A retract and keep
some solvent in the nozzle tip
Extruder A become idle
Extruder B purged out solvent in the tip
Extruder B become active
Finished one layer
Nozzle A&B moved into solvent
Extruder B retract and keep
some solvent in the nozzle tip
Further concern:
Paste dried on the way
back to solvent bath,
Especially for organic
solvent-based paste.

## Slide 15
3. Part deformation
Before sintering
After sintering
(ZrO2 substrates, Al2O3 traces)
Before sintering
After sintering
Dielectric substrates)

## Slide 16
Issues observed when using Al2O3 and ZrO2:
1. Undried conductive paste mixed with dielectric paste.
2. Dissimilar materials separate
during sintering.
Real LTCC pastes dries fast, and are
compatible for sintering。

## Slide 17: THANK YOU!